## Slide 1: Tutorial 1 Learning Topology Optimization Through Examples and Case Studies
August 18, 2019

## Slide 2
Cost-Effective Functional Designs for Additive Manufacturing

## Slide 3: Outline
Support structure constraint
Anisotropic strength
A. M. Mirzendehdel and K. Suresh, “Support structure constrained topology optimization for additive manufacturing”, Computer-Aided Design, vol. 81, pp. 1–13, 2016.
A. M. Mirzendehdel, B. Rankouhi, and K. Suresh, “Strength-based topology optimization for anisotropic parts”, submitted to Additive Manufacturing, 2016.

## Slide 4: Reducing support in TO
fabrication time
material usage
Reducing Support in AM Parts
clean-up time
Reduction in:
“… there will probably be instances where it is not necessary for all support structure to be eliminated and so the user should be able to have some control over the strength of the penalty function.” (Brackett et. al 2011 )

## Slide 5: Proposed
Support structure volume must be reduced during optimization
What is the impact on Performance?
but …
First optimize without support structure constraint
Support Volume Evaluation
Performance Evaluation
What is a reasonable constraint on Support?

## Slide 6: Lagrangian
Sensitivity field for Compliance
Sensitivity field for Support
Combination
Where to remove material?
Find sensitivity of the design to hypothetical infinitesimal change!

## Slide 7: Support Sensitivity Analysis
Interior
Support depends on
Local Normal
Length
Overhang Point
Support Point
Boundary
Threshold angle

## Slide 8: Constrained vs. Unconstrained
Unconstrained
Volume fraction = 0.5
Chart: Volume Fraction
| 0.5 | 0.52 | 0.54 | 0.56000000000000005 | 0.57999999999999996 | 0.6 | 0.63 | 0.65 | 0.68 | 0.7 | 0.72 | 0.75 | 0.77 | 0.8 | 0.82 | 0.85 | 0.87 | 0.9 | 0.92 | 0.95 | 0.97 | 1
Unconstrained | 1.29 | 1.24 | 1.2 | 1.16 | 1.13 | 1.1 | 1.08 | 1.06 | 1.045 | 1.03 | 1.025 | 1.02 | 1.016 | 1.013 | 1.009 | 1.005 | 1.004 | 1.003 | 1 | 1 | 1 | 1
Constrained(eta=0.50) | 1.58 | 1.51 | 1.46 | 1.42 | 1.385 | 1.35 | 1.32 | 1.28 | 1.25 | 1.22 | 1.19 | 1.16 | 1.13 | 1.09 | 1.06 | 1.04 | 1.02 | 1.01 | 1 | 1 | 1 | 1
Chart: Volume Fraction
| 0.5 | 0.52 | 0.54 | 0.56000000000000005 | 0.57999999999999996 | 0.6 | 0.63 | 0.65 | 0.68 | 0.7 | 0.72 | 0.75 | 0.77 | 0.8 | 0.82 | 0.85 | 0.87 | 0.9 | 0.92 | 0.95 | 0.97 | 1
Unconstrained | 5.06 | 4.69 | 4.18 | 3.67 | 3.46 | 3.03 | 2.8 | 2.7 | 2.64 | 1.61 | 1.32 | 0.9 | 0.9 | 0.9 | 1.41 | 1.46 | 1.41 | 1.03 | 0.79 | 0.79 | 0.79 | 0.79
Constrained(eta=0.50) | 2.43 | 2.04 | 2.06 | 1.63 | 1.14 | 1.03 | 0.91 | 0.79 | 0.79 | 0.79 | 0.79 | 0.79 | 0.83 | 0.79 | 0.79 | 0.79 | 0.79 | 0.79 | 0.79 | 0.79 | 0.79 | 0.79

## Slide 9: Constrained vs. Unconstrained
 | J/J0 | S (cm3)
Unconstrained | 1.24 | 5.46
Constrained | 1.58 | 2.21
 | 27% | 60%
Unconstrained
Volume fraction = 0.5

## Slide 10: Performance Tradeoff
Support volume reduced by about 17%
Volume fraction = 0.7
Compliance is increased by 137%
May not be possible !

## Slide 11: Outline
Support structure constraint
Anisotropic strength
A. M. Mirzendehdel and K. Suresh, “Support structure constrained topology optimization for additive manufacturing”, Computer-Aided Design, 2016.
A. M. Mirzendehdel, B. Rankouhi, and K. Suresh, “Strength-based topology optimization for anisotropic parts”, submitted to Additive Manufacturing, 2016.

## Slide 12: Introduction
Build
direction
Fused Deposition Modeling
Metal AM
“Incorporating … FDM processing to enhance strength … would significantly enhance a design optimization ...”
(Riddick et. al 2016)
“Metal fabrication processes rarely produce isotropic materials...”
(Luecke and Slotwinski 2014)
Constitutive Properties
(relating stress and strain)
Anisotropy
Directional Strengths

## Slide 13: Anisotropic Failure Criteria
Tsai-Wu Criterion:
Stress components are normalized w.r.t strength components.
Difference in compression vs. tension
Isotropic
von Mises Stress
No directional preference
Anisotropic
Tsai-Wu Criterion
directional preference

## Slide 14: Anisotropic Failure Criteria
Acceptable if less than 1
Only determines if the part fails or not!
Normalizing w.r.t strength

## Slide 15: Anisotropic Strength Ratio
Determine safety factor?
Simplest case: inverse of uniaxial stress
Tsai-Wu (Mixed order) : solution of quadratic equation
Maximize strength ratio
or safety factor
Measure strength

## Slide 16: Formulation
To avoid pathological conditions
Discretized approximation

## Slide 17: Anisotropic Strength Sensitivity Analysis

## Slide 18: Experiments
Material properties for ABS plastic at raster orientation of
Material strength components
Printer setup
XYZ Da Vinci Duo
90% infill density (maximum)
Tensile actuator setup
MTS Criterion Model 43
5KN load cell
Run at 5 mm/min
Data collection at 100Hz
Fused Deposition Modeling:
Strength anisotropy along build direction under tension
Ahn et al. (2002)
Riddick et al. (2016)
Ahn et al. (2003)

## Slide 19: Stiffness vs. Strength – Numerical solution
Reduce weight by 80%
Strength
Stiffness

## Slide 20: Stiffness vs. Strength – Experiments

## Slide 21: VonMises vs. Tsai-Wu – Numerical solution
Tension
Compression
Load
Load
vonMises (Isotropic)
Tsai-Wu (Anisotropic)
Tsai-Wu (Anisotropic)

## Slide 22: VonMises vs. Tsai-Wu – Experiments
Tension
Compression
Load
Load

## Slide 23: Conclusion
Considered support constraint in TO by:
  Posing the constraint w.r.t unconstrained TO
  Considering tradeoff with performance
Considered strength anisotropy in TO:
  Generalized Failure criteria such as Tsai-Wu
  Significant improvement in FDM parts via experimental tests

## Slide 24: Optimization method
Minimize {Volume, Compliance}
Constraint on displacement, stress,…
Constraint on support volume (*)
Challenging!
Not explored in literature!
Method: Pareto tracing
K. Suresh, “Efficient generation of large-scale pareto-optimal topologies,” Struct Multidisc Optim, vol. 47, no. 1, pp. 49–61, May 2012.
Optimal trade-off between objectives and constraints
Valid intermediate designs
Can make predictions throughout optimization

## Slide 25: Sensitivity Analysis
Take derivative of p-Norm
w.r.t Nodal Solution u
Solve Adjoint problem
Compute element sensitivity
Change in Quantity of Interest
Change in Compliance